## Slide 1
In order to achieve a continuous feedstock supply for power plants a large quantity of harvested material must be stored for long-term periods. During storage, especially during right conditions of temperature, moisture and oxygen, solid agricultural fuels are susceptible to microbial activities. Microbial respiration not only leads to loss of organic carbon, but also to an increased temperature in the stored fuel which may lead to self-ignition.
There is on-going work studying the effect of adding Ca as CaO or CaCO3 during storage of straw with the aim of creating an unfavorable alkaline microenvironment that prevents microbial growth during storage. The effect of this amendment during storage is still being explored, but the effect in the combustion step of the process in terms of determining the potential of Ca-additives to positively affect overall ash chemistry have yet to be certainly quantified.
Utilization of agricultural crops for energy purposes in heat and power plants has proven to be challenging in numerous ways. Compared to woody fuels, agricultural fuels can cause severe ash-related operational problems in combined heat and power plants through by fouling, slagging and/or bed agglomeration due to their high concentrations of inorganic constituents.
The objective of the present study is therefore to determine the fouling and bed agglomeration characteristics during fluidized-bed combustion of barley straw stored with different dosages of Ca to biomass with the main ash-forming elements shown in Figure 1, using two types of bed materials, quartz and olivine.
Chart: Mole/kg db
| K | Na | Ca | Mg | Fe | Al | Si | P | S | Cl
Barley | 0.28134 | 0.0032188 | 0.12476 | 0.027566 | 0.001343 | 0.0014455 | 0.18159 | 0.013237 | 0.023082 | 0.043724
Barley low | 0.28134 | 0.0031318 | 0.34932 | 0.032504 | 0.0025069 | 0.0020015 | 0.2528 | 0.016143 | 0.012789 | 0.048237
Barley high | 0.30692 | 0.0040453 | 0.57388 | 0.037852 | 0.0019697 | 0.0020015 | 0.2172 | 0.017757 | 0.025265 | 0.067137
Figure 1. Fuel fingerprint for used fuels.
INTRODUCTION
METHODOLOGY
Grain size of quartz and olivine bed materials used were 200-250 μm
Particulate Matter (PM)
Bed Ash
Cyclone Ash
Bed Grains
Gas
Measurements
Deposits Build-up on Deposition Probe
Samples collected both at the end of combustion and after agglomeration test
Elemental analysis – Scanning electron microscopy (SEM) with Energy Dispersive X-ray Spectroscopy (EDS)
Elemental analysis was carried out using a Zeiss EVO-LS15 equipped with a X-MmaxN 80 mm2 EDS detector
Fourier-transformed infrared spectroscopy (FTIR)
Gas measurements performed using a Gasmet DX-4000 FTIR
Barley straw
Barley straw
Low dosage of Ca-additive
Barley straw
High dosage of Ca-additive
Pelletized barley straw stored with Ca-additive
Combustion in bubbling fluidized bed in bench-scale (5 kW)
Analyses performed
1 Swedish University of Agricultural Sciences, Department of Forest Biomaterials and Technology, S-901 83 Umeå, Sweden
2 Umeå University, Department of Applied Physics and Electronics, Thermochemical Energy Conversion Laboratory, S-901 87 Umeå, Sweden
3 Luleå University of Technology, Energy Engineering, Division of Energy Science, SE-971 87 Luleå, Sweden
Combustion characteristics of barley straw stored with CaCO3 during fluidized bed
combustion using quartz and olivine as bed materials
Marjan Bozaghian1,*, Anders Rebbling2, Sylvia H. Larsson1, Shaojun Xiong1, Nils Skoglund2,3
CONCLUSIONS
Ca addition decreased the amount of alkali interaction between bed ash and bed material
Ca decreased the amount of molten bed ash particles discovered using SEM analysis
Release of gaseous K compounds due to tertiary ash transformation reactions may cause issues with deposition
Addition of Ca to barley straw causes significantly elevated CO concentrations in the flue gases regardless of bed material
Research financed by
PRELIMINARY RESULTS
Table 1 show indications that CO levels increases with added Ca. As the content of Ca is increasing, K-containing species are driven out and evaporates to the gas phase. Most likely, CO-levels are affected by the increase of gaseous K compounds in the flue gases.
Table 1. Gas measurements data based on average values from 8 hours combustion at 700 °C.
Gas measurements
Barley + quartz
Barley + olivine
Barley low+ olivine
Barley low+ quartz
Barley high + olivine
Barley high + quartz
Chart: Mole (%)
| K | Na | Ca | Mg | Fe | Al | Si | P | S | Cl
Barley + olivine | 26.8175 | 0.395 | 28.795 | 5.085 | 0.6725 | 0.18 | 26.79 | 2.3175 | 3.515 | 5.28
Barley low + olivine | 18.7875 | 0.425 | 47.205 | 3.8425 | 0.5175 | 0.665 | 19.885 | 1.81 | 2.41 | 4.02
Barley high + olivine | 12.725 | 0.7325 | 58.2175 | 3.42 | 0.245 | 0.2525 | 16.0275 | 1.4225 | 2.555 | 3.8925
Barley + quartz | 22.64 | 0.92 | 30.8567 | 4.7367 | 0.41667 | 0.68667 | 25.46 | 2.5867 | 4.15 | 7.0967
Barley low + quartz | 23.905 | 0.495 | 43.035 | 2.915 | 0.1225 | 0.1775 | 21.1625 | 1.5525 | 2.635 | 3.73
Barley high + quartz | 16.125 | 0 | 55.97 | 2.44 | 0.935 | 0 | 14.96 | 1.2025 | 1.945 | 4.6725
Area analysis of the cyclone ash particles, analysed with SEM-EDS analysis, show that in all fuels the cyclone ash was dominated by K, Ca and Si (Figure 2). It is also evident that a large proportion of the added Ca is trapped in cyclone ash which also appears to have an alkali reducing effect through dilution.
SEM-images of typical cyclone ash particles formed during combustion
Figure 2. Elemental composition of cyclone ash particles.
b) Quartz bed grains after combustion of 100% Barley
a) Olivine bed grains after combustion of 100% Barley
It is evident that olivine bed grains are more resistance to formation of particle layers than quartz bed grains in fluidized-bed combustion of pure barley straw.
No distinguishable layers could be observed in the case of olivine, whereas for quartz grains, molten ash particles adhered to bed particle grains could be observed (Figure 3).
SEM-images of typical cross section of olivine and quartz bed particles
Figure 3. Typical cross section of olivine and quartz bed particles taken after 8 h before agglomeration test.
 | Barley Quartz |  | Barley Olivine |  | Barley low Quartz |  | Barley low Olivine |  | Barley high Quartz |  | Barley high Olivine | 
 | Average | StdDev | Average | StdDev | Average | StdDev | Average | StdDev | Average | StdDev | Average | StdDev
Temp | 695,7 | 4,4 | 691,9 | 9,7 | 690,5 | 6,6 | 687 | 11,7 | 701,9 | 3,3 | 716,6 | 8,8
CO [ppm] | 69,7 | 56,1 | 12 | 39,5 | 6214,8 | 3709,1 | 1851,8 | 1767,5 | 5393,9 | 2377,9 | 6345,5 | 3504,1
O2 [% dry] | 12,6 | 1,1 | 11,6 | 2,1 | 10,4 | 4,2 | 14,7 | 2,5 | 12,8 | 1,7 | 11,3 | 2,4
*)corresponding author, . E-mail: marjan.bozaghian@slu.se